TJ4 Factory 139788 step3 Equipment Material Conveying Pipeline Quality Inspection Scheme & Risk Assessment of Reporting Unsatisfactory Items /

TJ4厂区139788 step3设备物料输送管路质量检测方案&报告不满足项风险评估

Document No. /文件编号：RA-TJ42026063.01

| Prepared by /起草人 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Fengjiang Li/李丰江 (Junior Engineer, Production/初级工程师，生产部) | Signature/ 签名 |  | Date/ 日期 |  |
| Reviewed by/复核人 |  |  |  |  |
| Xingtao Fan/范兴涛 (Senior Director, Production/高级主管，生产部) | Signature/签名 |  | Date/日期 |  |
| Hui Ma /马辉 (Senior Director, Production/高级主管，生产部) | Signature/签名 |  | Date/日期 |  |
| Qi Wang/王琪 (Senior Director, QA/高级主管，QA) | Signature/签名 |  | Date/日期 |  |
| Approved by/审批人 |  |  |  |  |
| Shenghui Yu/于生辉 (Vice General Manager, QA/副总经理，QA) | Signature/签名 |  | Date/日期 |  |

Table of Content/目录

1. Objective/目的	3

2. Scope /范围	3

3. Risk assessment /风险分析	3

3.1 Non-compliance Item 1: Assessment of the Non-BPE Piping of the 139788 step3 Preparation Solution System and Preparation System Piping;	4

3.1 不满足项1：139788 step3制备配液系统及制备系统管路是非BPE管路的评估；	4

3.2 Non-compliance Item 2: Situation Where Multiple Tees, Crosses and Other Positions of Piping Do Not Meet the 2D Requirement;	9

3.2 不满足项2：管路多个三通、四通等位置不满足2D的情况；	9

3.3 Non-compliance Item 3: Situation Where Diaphragm Valve Installation Angle Does Not Meet Self-Draining Requirement.	13

3.3 不满足项3：隔膜阀安装角度不满足自排尽的情况。	13

4.Conclusion /小结	15

5.Revision History /修订历史	16

1. Objective/目的

Asymchem Life Science (Tianjin) Co., Ltd. (No. 265, South Street, Economic-Technological Development Area, Binhai New Area, Tianjin, China) (hereinafter referred to as the "TJ4 site") is a multi-purpose manufacturing plant designed for the production of various intermediates and APIs. The equipment and facilities employed for the production of intermediates and APIs are non-dedicated and are adaptable for campaign-based manufacturing of multiple products./

凯莱英医药集团（天津）股份有限公司（中国天津市滨海新区经济技术开发区南大街265号）（简称TJ4厂区）是一家多用途生产工厂，旨在生产不同的中间体和API。用于生产中间体和 API 的设备和设施是非专用的，可适配多品种产品阶段性生产。

The purpose of this risk assessment is to systematically evaluate the unsatisfied items in the quality inspection plan & report (SVP-TJ4-183.01-004) of the material conveying pipeline of 139788 step3 equipment./

该风险评估的目的是对139788 step3设备物料输送管路质量检测方案&报告（SVP-TJ4-183.01-004）不满足项开展系统性评估。

2. Scope /范围

This appraisal document is applicable to the systematic appraisal of the unsatisfied items in the quality inspection plan & report (SVP-TJ4-183.01-004) of 139788 step3 material conveying pipeline of Gloria Pharmaceutical Group (Tianjin) Co., Ltd. (No.265, South Street, Economic and Technological Development Zone, Binhai New Area, Tianjin, China). There are mainly three aspects that can not meet the requirements of the corresponding BPE standard, namely: 1.139788 step3 Evaluation of the preparation liquid preparation system and the pipeline of the preparation system as non-BPE pipeline; 2. The condition that multiple tees, tees and tank mouths of equipment and pipelines do not meet the requirements of 2D, and 3. The installation angle of diaphragm valve does not meet the requirements of self-exhaustion./

本评估文件适用于凯莱英医药集团（天津）股份有限公司（中国天津市滨海新区经济技术开发区南大街265号）（简称TJ4厂区）的139788 step3物料输送管路质量检测方案&报告（SVP-TJ4-183.01-004）不满足项开展系统性评估。主要是三个方面的不能满足对应BPE标准要求，分别是：1.139788 step3制备配液系统及制备系统管路是非BPE管路的评估；2.设备、管路多个三通、四通、罐口不满足2D的情况，3.隔膜阀安装角度不满足自排尽的情况。

3. Risk assessment /风险分析

The 139788step3 process pipeline is mainly used for system or solution transfer between devices in this step, and the process solution can be transferred in a closed way in the pipeline. At present, the pipeline is mainly made of 316L stainless steel with different specifications, and some of them are made of Hastelloy. Most of the process pipelines adopt quick-opening connection mode, including standard straight pipes with a length less than 2m. The pipeline system also includes corresponding standard quick-opening elbows, tees, four-way, etc., and valves, flowmeters, pumps, hoses and other designs are arranged in the pipeline to realize material transfer control and control residues to the greatest extent. Through the corresponding cleaning methods in and after the project batch, the pipeline can be effectively cleaned to avoid cross-contamination and control the load of microorganisms and endotoxin. Some of the hoses are lined with tetrafluoroethylene and the inner surface is smooth, which can meet the requirements of material compatibility and residue control.

139788step3工艺管路主要是该步骤各个设备之间用于体系或溶液转移使用，工艺溶液在管道内可以实现密闭转移。目前管路的材质主要是不同规格的316L不锈钢的材质，部分为哈氏合金材质，工艺管路多数采用快开的连接方式，含标准的长度小于2m的直管，管路系统中还包含有对应标准快开弯头、三通、四通等部件，管路中设置有阀门、流量计、泵、软管等设计，以实现物料的转移控制，并最大程度的控制残留。项目批次内、结束后通过对应的清洗方法，实现对管路的有效清洁，避免交叉污染、控制微生物和内毒素负载。其中部分软管为内衬四氟且内表面光滑的形式，可以满足物料的材质兼容性要求残留的控制要求。

In the 139788 step3 process piping, the national standard (ISO) piping adopts manual welding, while the BPE piping adopts automatic welding. All corresponding pipes undergo passivation work before use and piping validation work (Material Transfer Piping Quality Inspection Plan & Report (SVP-TJ4-183.01-004)). This document mainly conducts risk analysis on three aspects of non-compliance to ensure the corresponding risks are controllable, and formulates short-term and long-term measures./

139788step3工艺管路中ISO标准管路采用手动焊接的形式，BPE管路采用自动焊接的形式，对应管道均进行对应的使用前的钝化工作及管道验证工作（物料输送管路质量检测方案&报告（SVP-TJ4-183.01-004），本文件主要是针对三个方面的不满足的情况进行FMEA风险分析，以确保对应风险可控，并制定短期和长期的措施。

Description of FMEA scoring standard:/FMEA评分标准说明：

· Severity (s): 1 = negligible; 3= moderate impact (rework required/yield decreased); 4= serious impact (affecting key quality attributes of products/leading to batch suspension); 5= catastrophic (quality and safety/regulatory violations).

严重度（S）：1=可忽略；3=中等影响（需返工/收率下降）；4=严重影响（影响产品关键质量属性/导致停批）；5=灾难性（质量安全/法规违规）。

· Probability of occurrence (p): 1 = rare occurrence (< 1%); 3= Occasional (1-10%); 4= Frequent occurrence (10-30%); 5= Frequent occurrence (> 30%).

发生概率（P）：1=极少发生（<1%）；3=偶尔发生（1-10%）；4=经常发生（10-30%）；5=频繁发生（>30%）。

· Detectability (D): 1 = almost certainly detectable (e.g. 100% endoscope+physical and chemical detection); 3= There is a moderate chance of detection (such as visual inspection by random inspection); 5= Almost impossible to detect (e.g. only by final product inspection).

可检测度（D）：1=几乎肯定能检出（如100%内窥镜+理化检测）；3=有中等机会检出（如抽检目视）；5=几乎无法检出（如仅靠终产品检验）。

· Risk grade determination: RPN ≤ 12 (low risk, acceptable); 12 < RPN ≤ 24 (medium risk, need control measures); RPN > 24 (high risk, must be rectified/require special approval from QA).

风险等级判定：RPN ≤ 12（低风险，可接受）；12 < RPN ≤ 24（中风险，需控制措施）；RPN > 24（高风险，必须整改/需QA特批）。

（RPN＝S×P×D）

3.1 Non-compliance Item 1: Assessment of the Non-BPE Piping of the 139788 step3 Preparation Solution System and Preparation System Piping;

3.1 不满足项1：139788 step3制备配液系统及制备系统管路是非BPE管路的评估；

Specific Situation:

具体情况：

Due to the long delivery lead time of BPE piping, temporary use was made for the early Demo batches of this 139788 step3 piping. After the subsequent BPE piping arrives, re-manufacturing and installation will be carried out. A comprehensive comparison and risk analysis between the existing ISO piping and BPE piping will be conducted to confirm whether it meets project production use.

本次139788step3管路因BPE管路到货周期较长，临时进行前期Demo批次的使用，待后续BPE管路到货后进行重新制作安装，对应现有的ISO管路和BPE管路进行整体的对比和风险分析，确认是否满足项目生产使用。

Specific Piping List:

具体管路清单：

| Pipeline number/管路编号 | Specifications/规格 | texture of wood/材质 | executive standard/执行标准 |
| --- | --- | --- | --- |
| 139788-step3B-P06 | DN25 | 316L | ISO |
| 139788-step3B-P07 | DN25 | 316L | ISO |
| 139788-step3B-P04 | DN25 | 316L | ISO |
| 139788-step3B-P01 | DN50 | 316L | ISO |
| 139788-step3B-P02 | DN25 | 316L | ISO |
| 139788-step3B-P03 | DN25 | 316L | ISO |
| 1211-FD01-P01 | DN40 | 316L | ISO |
| 1211-FD01-P01 | DN25 | 316L | ISO |
| 1211-AT01-P01 | DN25 | 316L | ISO |
| 1211-HPPC03-T04-P01 | DN25 | 316L | ISO |
| Acetonitrile pipeline/乙腈管路 | DN50 | 316L | ISO |
| 1211-HPPC03-T02-P02 | DN25 | 316L | ISO |
| 1211-HPPC03-T04-P01 | DN25 | 316L | ISO |
| 1211-HPPC03-T05-P02 | DN25 | 316L | ISO |
| 1211-HPPC03-T02-P04 | DN40 | 316L | ISO |
| 1211-HPPC03-T06-P03 | DN25 | 316L | ISO |
| 1211-HPPC03-T05-P01 | DN25 | 316L | ISO |
| 1211-HPPC03-AT01-P02 | DN25 | 316L | ISO |
| 1211-HPPC03-T01-P04 | DN25 | 316L | ISO |
| 1211-HPPC03-T01-P03 | DN25 | 316L | ISO |
| 1211-HPPC03-T02-P03 | DN25 | 316L | ISO |
| 1211-HPPC03-T02-P02 | DN25 | 316L | ISO |
| 1211-HPPC03-AT04-P03 | DN25 | 316L | ISO |
| 139788-step3A-P06 | DN25 | 316L | ISO |
| 1211-HPPC03- P04 | DN25 | 316L | ISO |
| 1211-HPPC03- P01 | DN25 | 316L | ISO |
| 139788-step3A-P04 | DN25 | 316L | ISO |
| 1211-HPPC03-AT03-P02 | DN25 | 316L | ISO |
| 1211-HPPC03-AT06-P02 | DN25 | 316L | ISO |

Risk Analysis:

风险分析：

A systematic assessment is conducted on core technical requirements such as material, welding, acid pickling passivation, and tolerance diameter, based on the ISO standard system requirements and referencing ASME BPE-2026 (Bioprocessing Equipment Standard, June 2026). The assessment follows ISO management requirements and covers the following core equipment and facility components: piping, pipe fittings, valves, pumps, and all surface treatment links in contact with the product. The assessment includes core requirements for material, welding, acid pickling passivation, tolerance diameter, and surface finish.

从材质、焊接、酸洗钝化及公差直径等核心技术要求进行系统性评估，依据ISO 标准体系要求，参考ASME BPE-2026（生物工艺设备标准，2026年6月），评估以 ISO 管理要求，评估涵盖以下核心设备设施组件：管道、管件、阀门、泵，以及与产品接触的所有表面处理环节。评估包涵材质、焊接、酸洗钝化、公差直径、表面光洁度核心要求。

Material Requirements Assessment: Product contact surfaces are all based on 316L as the benchmark; non-contact surfaces can be downgraded to 304/304L. All the above related materials are provided with material certificates including material content. The requirements are basically consistent between ISO and ASME BPE-2026.

材质要求评估：产品接触面均以316L为基准，非接触面可降级至304/304 L，以上相关材料均提供材质证明包含材料含量，ISO和ASME BPE-2026要求基本一致。

Evaluation of welding requirements: 99.997% of welding gas meets argon protection requirements after detection, with automatic welding as the priority and manual welding as the auxiliary. The detection ratio is ≥20% for automatic weld inspection, 100% for manual weld inspection, and the 2D dead angle rule L/D is ≤ 2: 1. The product contact surface is not allowed to meet the requirements of blowholes, undercut and welding slag, etc., ISO and ASME BPE-2026. The qualification of welding personnel is the government special operation certificate.

焊接要求评估：焊接气体经过检测99.997%满足氩气保护要求，焊接方法以自动焊接优先为主，手动焊接为辅助，检测比例自动焊缝 ≥20%内窥镜检查，手动焊缝100%内窥镜检查，2D死角规则L/D ≤ 2:1，产品接触面不允许气孔、咬边、焊渣等要求，ISO和ASME BPE-2026要求基本一致，且针对ISO标准管材的验收以ASME BPE-2026的要求为标准。焊接人员资质为政府特种作业操作证。

This paper evaluates the inconsistency of pipeline system which adopts ISO standard pipes and is accepted according to ASME BPE. In welding, there are deviations between ISO pipes and BPE requirements in sulfur content, dimensional tolerance and end face quality, which may lead to defects such as insufficient fluidity, incomplete fusion, porosity, hot cracks or mismatching. As for the roughness of inner wall, ISO pipes usually only specify Ra value, while BPE has systematic requirements for surface smoothness of SFF1-SFF6, and high roughness will affect CIP/SIP effect. In view of the above risks, the following control measures are taken: 100% check the outer diameter, wall thickness and ovality of the pipe end, and control the wrong side; Re-evaluate the welding procedure with this batch of pipes, lock the welding parameters and record each joint; The sampling rate of automatic welding endoscope is 20%, and manual welding endoscope is 100%; The manufacturer provides the roughness test report for the inner wall roughness, and our company checks and accepts it according to BPE standard. Combined with cleaning verification and surface sampling monitoring, the welding defects and cleaning risks caused by the difference between ISO pipe and BPE standard can be effectively reduced. Therefore, the scheme is technically feasible and the differential risk is acceptable under controlled conditions./

针对采用ISO标准管材按ASME BPE验收的管道系统不一致方面评估。焊接方面，ISO管材在硫含量、尺寸公差和端面质量与BPE要求存在偏差，可能导致轨道焊熔池流动性不足、未熔合、气孔、热裂纹或组对错边等缺陷。内壁粗糙度方面，ISO管材通常仅规定Ra值，而BPE对表面光洁度有SFF1–SFF6体系化要求，粗糙度偏高会影响CIP/SIP效果。针对上述风险采取以下控制措施：100%复核管端外径、壁厚及椭圆度，控制组对错边；使用本批管材重新进行焊接工艺评定，锁定焊接参数并记录每道焊口；自动焊内窥镜抽检比例20%，手工焊100%内窥镜检查；内壁粗糙度由厂家提供粗糙度检测报告，我司以BPE标准进行核查验收，结合清洁验证及表面取样监测，可有效降低ISO管材与BPE标准差异带来的焊接缺陷和清洁风险。因此，该方案在受控条件下技术可行，差异风险可接受。

Acid Pickling Passivation Requirements Assessment: There are acid pickling passivation plans, acid pickling passivation records, post-passivation test results, and polishing standards. Requirements are basically consistent between ISO and ASME BPE-2026.

酸洗钝化要求评估：有酸洗钝化方案、酸洗钝化记录、酸洗钝化后检测结果和抛光度标准，ISO和ASME BPE-2026要求基本一致。

Tolerance and Diameter Requirements Assessment: Pipe connections use clamp quick connections, pipe slope satisfies >=1%, inner surface roughness in direct contact with product satisfies <=0.4um. Requirements are basically consistent between ISO and ASME BPE-2026. Pipe diameter, tolerance, wall thickness, etc., are selected in combination with different process points using pipe materials meeting ISO or ASME BPE-2026 process requirements; process risk is acceptable./

公差与直径要求评估：管道连接卡箍快接、管道坡度满足≥1%、直接接触产品内表面粗糙度要求满足≤0.4 um，ISO和ASME BPE-2026要求基本一致，管道直径、公差、壁厚等结合工艺的不同点位选用满足ISO或ASME BPE-2026工艺需求的管材，工艺风险可接受。

Control Measures:

控制措施：

Short-term Measures: The overall management requirements for piping shall be consistent with BPE piping, supporting the production of the 139788 step3 Demo batch./

短期措施：管路整体管理要求同BPE管路一致，支持139788 step3 Demo批次的生产。

Long-term Measures: Complete the re-design and installation validation of BPE piping before the 139788 step3 Pre-PPQ, subsequently serving as the dedicated piping for this project./

长期措施：在139788 step3 Pre-PPQ前完成BPE管路的重新设计及安装验证工作，后续作为该项目的专用管路。

Targeted evaluation form FMEA/针对性FMEA评估表：

| Failure mode/失效模式 | Potential impact/潜在影响 | Before taking measures/措施前 |  |  |  |  | Control measure/控制措施 | After the measures/措施后 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | S | P | D | RPN | Risk level/风险等级 |  | S | P | D | RPN | Risk level/风险等级 |
| ISO/BPE hybrid welding produces staggered edges and incomplete fusion. / ISO/BPE混杂焊接产生错边、未熔合 | Affect the welding quality, which may lead to cleaning dead corners./ 影响焊接质量，可能导致清洁死角 | 2 | 3 | 3 | 18 | Medium risk/中风险 | 100% recheck the pipe end size and control the wrong side; 100% endoscopic inspection of ISO-BPE butt weld; Re-evaluate the welding procedure / 100%复核管端尺寸，控制错边；ISO-BPE对接焊缝100%内窥镜检查；重新进行焊接工艺评定 | 1 | 2 | 2 | 4 | Low risk/低风险 |
| The sulfur content of ISO pipeline is different from that of BPE standard, which affects the welding quality. / ISO管道硫含量与BPE标准存在差异，影响焊接质量 | It may lead to defects such as insufficient fluidity of molten pool, blowhole, hot crack and incomplete fusion, which will affect weld quality and cleaning risk./ 可能导致熔池流动性不足、气孔、热裂纹、未熔合等缺陷，影响焊缝质量及清洁风险 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Check the sulfur content in the pipe material certificate, and retest by batch if necessary; 100% recheck the pipe end size and control the wrong side; Re-evaluate the welding process with this batch of pipes and lock the welding parameters; 100% endoscopic inspection of ISO-BPE butt weld; 20% of automatic welding endoscopes were sampled and 100% of manual welding endoscopes were inspected./ 核查管材材质证书中硫含量，必要时按批次复测；100%复核管端尺寸，控制错边；使用本批管材重新进行焊接工艺评定，锁定焊接参数；ISO-BPE对接焊缝100%内窥镜检查；自动焊内窥镜抽检20%，手工焊100%内窥镜检查 | 2 | 2 | 2 | 8 | Low risk/低风险 |
| The difference of inner wall roughness affects CIP/SIP effect./ 内壁粗糙度差异影响CIP/SIP效果 | May affect the cleaning effect/ 可能影响清洁效果 | 2 | 1 | 2 | 4 | Medium risk/低风险 | The roughness test report of the inner wall is provided by the manufacturer, and our company checks and accepts it according to BPE standard, combined with cleaning verification and surface sampling monitoring./ 内壁粗糙度由厂家提供粗糙度检测报告，我司以BPE标准进行核查验收，结合清洁验证及表面取样监测。 | 2 | 1 | 2 | 4 | Low risk/低风险 |

Conclusion:

结论：

After systematic evaluation, all pipes are accepted according to ASME BPE-2026 requirements, forming a complete standard group in terms of welding procedure qualification, welder qualification and welding acceptance grade, providing an executable main framework, covering core management elements such as materials, welding methods and qualifications, basic requirements for passivation, drainage slope, dead angle rules and surface roughness, etc. The risk of difference is controllable, so it can be directly used as the basis for implementation, and the risk of project use is low./

经系统评估，以ASME BPE-2026要求标准对所有的管材进行验收，在焊接工艺评定、焊工资格、焊接验收等级方面形成了完整的标准群，提供了可执行的主框架，覆盖材质、焊接方法与资格、钝化基本要求、排水坡度、死角规则与表面粗糙度等核心管理要素，差异风险可控，故可直接作为执行依据，项目使用风险较低。

3.2 Non-compliance Item 2: Situation Where Multiple Tees, Crosses and Other Positions of Piping Do Not Meet the 2D Requirement;

3.2 不满足项2：管路多个三通、四通等位置不满足2D的情况；

Specific Situation:

具体情况：

According to the ASME BPE standard SJ-03 chapter Dead Leg control requirements:/

根据ASME BPE标准SJ-03章节死腔（Dead Leg）管控要求：

In clean fluid systems, for all non-continuous flow branches (tee branches, instrument interfaces, sampling ports, drainage ports, plugs, etc.), the ratio of the length L from the inner wall of the main pipeline to the blind end of the branch, to the branch's own inner diameter d must satisfy L/d <= 2 (i.e., the 2D requirement)

洁净流体系统中，所有非连续流支路（三通分支、仪表接口、取样口、排放口、堵头等），从主管路内壁到支路盲端的长度L，与支路自身内径d的比值需满足 L/d ≤ 2（即2D要求）

Due to the long delivery lead time of short-radius tees, T-type valves, zero static valves, GMP diaphragm valves, etc., this 139788 step3 piping was manufactured using general fittings, resulting in some components not meeting the 2D requirement, which was identified during the piping validation process; the specific list is shown in the table below:

本次139788step3管路因短径三通、T型阀、零静态阀门、GMP隔膜阀等货期较长，使用一般配件进行管路的制作，存在部分部件不能满足2D的情况，在管路验证过程中进行识别，具体清单见下表：

| P&ID No. of component 部件号 | 使用原则 (mm:mm) | L=L0+e1 | d=d0-2e2 | L/d |
| --- | --- | --- | --- | --- |
| TJ4S-1211-FD01-V97 | L/d≤2 | 137.45mm | 27.17mm | 4.83 |
| TJ4S-1211-R01-VS4 | L/d≤2 | 130.15mm | 22.06mm | 5.89 |
| TJ4S-1211-AT02-V23 | L/d≤2 | 124.66mm | 13.80mm | 9.03 |
| TJ4S-1211-AT02-V24 | L/d≤2 | 109.40mm | 12.88mm | 8.49 |
| TJ4S-1211-HPP/03-AT01-V15 | L/d≤2 | 118.74mm | 25.23mm | 4.70 |
| TJ4S-1211-HPP/03-T03-V21 | L/d≤2 | 143.80mm | 22.01mm | 6.53 |
| TJ4S-1211-HPP/03-AT04-V22 | L/d≤2 | 120.27mm | 25.73mm | 4.67 |
| TJ4S-1211-HPP/03-AT04-V24 | L/d≤2 | 119.97mm | 25.87mm | 4.64 |
| TJ4S-1211-TFF02-V31 | L/d≤2 | 123.25mm | 22.14mm | 5.56 |
| TJ4S-1211-HPP/03-AT02-V15 | L/d≤2 | 118.54mm | 26.07mm | 4.54 |
| TJ4S-1211-HPP/03-AT02-V18 | L/d≤2 | 86.09mm | 12.25mm | 7.02 |
| TJ4S-1211-HPP/03-AT02-V14 | L/d≤2 | 118.74mm | 25.23mm | 4.70 |
| TJ4S-1211-HPP/03-T06-V09 | L/d≤2 | 118.98mm | 25.72mm | 4.60 |
| TJ4S-1211-HPP/03-T06-V17 | L/d≤2 | 120.10mm | 25.86mm | 4.64 |
| TJ4S-1211-TFF02-V105 | L/d≤2 | 101.59mm | 13.25mm | 7.66 |
| LY2607062J5 | L/d≤2 | 169.15mm | 25.24mm | 6.54 |
| LY260706226 | L/d≤2 | 172.23mm | 26.90mm | 6.40 |
| Y126070624 | L/d≤2 | 193.64mm | 26.77mm | 7.42 |
| CZH031507 | L/d≤2 | 198.08mm | 27.45mm | 7.21 |
| CZH031508 | L/d≤2 | 165.07mm | 12.56mm | 13.15 |
| CZH081498 | L/d≤2 | 170.73mm | 23.84mm | 6.60 |

Risk Analysis:

风险分析：

When L/d > 2, the turbulence of the main pipeline (CIP condition Reynolds number Re>=3000) cannot effectively entrain the fluid within the branch; a static retention dead zone forms inside the branch; the medium cannot circulate and renew, and cleaning fluid cannot effectively penetrate - this is the root cause of all risks./

当L/d＞2时，主管路的湍流（CIP工况雷诺数Re≥3000）无法有效夹带支路内的流体，支路内部形成静态滞留死区，介质无法循环更新，清洗液、无法有效穿透，是所有风险的根源。

Microbial pollution and biofilm risk: the fluid in the dead zone is still, and the pipeline is completely exhausted at low points after use, and nitrogen purging further reduces the residue. After the pipeline is used, carry out the circulation cleaning of each port to ensure that all the paths are cleaned. At the same time, dismantle the tee and other parts that do not meet 2D requirements for visual inspection and confirmation, and increase the circulation cleaning and wiping sampling of the dead zone of the side port, which can reduce the risk to a low level./

微生物污染与生物膜风险：死区内流体静止，管路在使用完毕后进行低点完全排尽、氮气吹扫进一步降低残留。管路使用完毕后进行各个口的流通式清洗，确保全部路径得到清洗，同时三通等不满足2D的部件进行拆卸进行目视检查确认，增加侧口死区流通式清洗、擦拭取样，可以将风险降到低风险；

CIP Cleaning Effectiveness Failure Risk: The turbulence of the main pipeline cannot be transmitted into the dead zone; cleaning fluid can only form a weak laminar exchange at the dead zone inlet and cannot effectively scour the inner wall; residual materials and cleaning agents cannot be completely displaced, forming permanent residual. Based on this risk, increase flow-through cleaning of the side port dead zones and perform visual inspection confirmation after disassembly, which can reduce the risk to low risk.

2. CIP清洗有效性失效风险：主管路的湍流无法传递至死区内部，清洗液仅能在死区入口形成微弱的层流交换，无法有效冲刷内壁；残留物料、清洁剂无法被完全置换，形成永久残留。根据该风险，增加侧口死区的流通式清洗，并做拆卸下来后的目视检查确认，可以将风险降到低风险。

Product Quality and Yield Risk: Product materials retained in the dead zone cannot be discharged with the main pipeline and remain after batch completion, causing fluctuations in critical quality attributes. Product retention loss leads to decreased product yield. Based on this risk characteristic, after project use, process solvent flushing and nitrogen purging are performed to avoid corresponding risks.

3. 产品质量与收率风险：死区内滞留的产品物料无法随主管路排出，批次结束后残留，造成关键质量属性波动。产品滞留损失，产品收率下降。根据该风险特征，项目使用结束后进行工艺溶剂的淌洗、氮气吹扫，避免对应风险。

Equipment Corrosion and Maintenance Risk: Liquid retained in the dead zone for a long time destroys the hygienic grade piping inner surface finish (Ra≤0.4um), causing pitting corrosion and crevice corrosion; corrosion products further aggravate retention and pollution. For this risk, timely complete drainage is performed after material and cleaning transfer is completed, and since the corresponding materials in this project are non-corrosive, the risk is low.

4. 设备腐蚀与运维风险：液体在死区内长期滞留，破坏卫生级管路内表面光洁度（Ra≤0.4μm），引发点蚀、缝隙腐蚀；腐蚀产物进一步加剧滞留与污染。针对该风险在物料以及清洗转移结束后进行及时排尽，且本项目中对应物料无腐蚀性，风险较低。

Control Measures:

控制措施：

Short-term Measures: Execute according to the risk assessment plan to support Demo batch production. Timely complete drainage through process solvent flushing and nitrogen purging; for cleaning, flow-through cleaning of each port is performed and disassembly for visual inspection is carried out; corresponding risks are controllable./

短期措施：按照风险评估的方案执行，支持Demo批次生产。通过工艺溶剂淌洗、氮气吹扫，及时排尽；清洗上，各个口流通式清洗，并拆卸进行目视检查，对应风险可控。

Long-term Measures: Before the Pre-PPQ batch, carry out equipment modification and dimensional optimization: shorten over-specification branch pipes and strictly control L/d<=2; replace positions that cannot be shortened with zero dead-leg tees or clamp-style flush joints to structurally eliminate retention cavities. And conduct re-validation confirmation of piping and equipment.

长期措施：在Pre-PPQ批次前进行设备改造，尺寸优化改造：对超标支管进行截短，严格控制L/d≤2；无法截短的位置更换为零死区三通、夹装式齐平接头，从结构上消除滞留腔。并进行管路和设备的再次验证确认。

Targeted evaluation form FMEA/针对性FMEA评估表：

| Failure mode/失效模式 | Potential impact/潜在影响 | Before taking measures/措施前 |  |  |  |  | Control measure/控制措施 | After the measures/措施后 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | S | P | D | RPN | Risk level/风险等级 |  | S | P | D | RPN | Risk level/风险等级 |
| Dead zone retention leads to microbial growth (water phase pipeline)/死区滞留导致微生物滋生（水相管路） | May breed microorganisms/可能滋生微生物 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Identify the list of water phase pipelines; Increase the side port dead zone circulation cleaning; Increase wiping sampling /识别水相管路清单；增加侧口死区流通式清洗；增加擦拭取样 | 2 | 2 | 2 | 8 | Low risk/低风险 |
| Failure of CIP cleaning effectiveness and material residue /CIP清洗有效性失效、物料残留 | Material residue, affecting cleaning./物料残留，影响清洁 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Disassembly does not meet the visual inspection of 2D parts; Increase physical and chemical detection of wiping sampling; Process solvent washing and nitrogen purging/拆卸不满足2D部件目视检查；增加擦拭取样理化检测；工艺溶剂淌洗、氮气吹扫 | 2 | 2 | 2 | 8 | Low risk/低风险 |
| Long-term detention leads to pipeline corrosion/长期滞留导致管路腐蚀 | May corrode the pipeline/可能腐蚀管路 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Drain it in time after use; Materials are non-corrosive; Periodic inspection/使用后及时排尽；物料无腐蚀性；定期检查 | 2 | 1 | 2 | 4 | Low risk/低风险 |

Conclusion:

结论：

The existing equipment can support Demo batch production. After the Demo batch, re-design and modify non-conforming piping, then conduct validation after modification, ensuring this non-compliance item is resolved before Pre-PPQ.

现有设备可以支持Demo批次的生产，Demo批次后对不合格的管路进行重新设计改造，改造后进行验证，确保在Pre-PPQ前解决该不满足项。

3.3 Non-compliance Item 3: Situation Where Diaphragm Valve Installation Angle Does Not Meet Self-Draining Requirement.

3.3 不满足项3：隔膜阀安装角度不满足自排尽的情况。

Specific Situation:

具体情况：

This assessment is based on ASME BPE standards: clean pipeline short pipe slope >=1%, valves must follow the pipeline slope to achieve self-draining; China GMP: pipeline design and installation should avoid dead corners and blind pipes to prevent microbial growth and ensure complete system drainage. In this validation, the essential reason why diaphragm valves do not meet the requirement is that self-draining of weir-type hygienic grade diaphragm valves depends on gravity action. When the installation angle does not meet the standard (level without slope, insufficient slope, or reverse slope), a permanent accumulated liquid dead zone forms at the bottom of the valve cavity, which is the root cause of all risks. The specific valve installation angle follows the manufacturer's equipment manual and is measured and confirmed one by one during piping validation. The following is a list of diaphragm valves identified during validation that do not meet the standard:

本次评估基于ASME BPE 标准：洁净管路短管坡度≥1%，阀门需顺应管路坡度实现自排净；中国GMP：管道设计安装应避免死角、盲管，防止微生物滋生，确保系统完全排放。在本次验证中隔膜阀不满足的本质是堰式结构卫生级隔膜阀的自排净依赖重力作用，安装角度不达标（水平无倾斜、倾斜不足、反向倾斜）时，阀腔底部会形成永久性积液死区，是所有风险的根源。具体阀门的安装角度依据厂家设备说明书执行，在管道验证中进行逐一测量确认。以下是在验证中识别的不满足标准的隔膜阀清单：

| Serial number/序号 | Valve number/阀门编号 | Factory/厂家 | Target angle/目标角度 | Current angle/当前角度 | Remarks/备注 |
| --- | --- | --- | --- | --- | --- |
| 1 | TJ4S-1211-TFF02-V60 | Nuomeng/诺盟 | 60° | 40.4° | The pipeline is blocked and cannot be adjusted./管路遮挡，无法调整 |
| 2 | TJ4S-1211-TFF02-V123 | Nuomeng/诺盟 | 60° | 38.9° | The pipeline is blocked and cannot be adjusted./管路遮挡，无法调整 |
| 3 | TJ4S-1211-HPPC03-AT05-V29 | Nuomeng/诺盟 | 60° | -90° | The valve hangs upside down and clings to the roof./阀门倒垂，紧贴顶板 |
| 4 | TJ4S-1211-HPPC03-AT06-V19 | Nuomeng/诺盟 | 60° | -90° | The valve hangs upside down and clings to the roof./阀门倒垂，紧贴顶板 |
| 5 | TJ4S-1211-HPPC03-AT06-V20 | Nuomeng/诺盟 | 60° | -90° | The valve hangs upside down and clings to the roof./阀门倒垂，紧贴顶板 |
| 6 | TJ4S-1211-HPPC03-AT06-V21 | Nuomeng/诺盟 | 60° | -90° | The valve hangs upside down and clings to the roof./阀门倒垂，紧贴顶板 |
| 7 | TJ4S-1211-HPPC03-AT06-V22 | Nuomeng/诺盟 | 60° | -90° | The valve hangs upside down and clings to the roof./阀门倒垂，紧贴顶板 |
| 8 | TJ4S-1211-R01-V03 | Nuomeng/诺盟 | 71° | 90° | The valve is vertical and clings to the top plate./阀门垂直，紧贴顶板 |
| 9 | TJ4S-1211-R01-V24 | Nuomeng/诺盟 | 64° | 90° | The valve is vertical and clings to the top plate./阀门垂直，紧贴顶板 |
| 10 | TJ4S-1211-R01-V25 | Nuomeng/诺盟 | 64° | 90° | The valve is vertical and clings to the top plate./阀门垂直，紧贴顶板 |
| 11 | TJ4S-1211-R01-V54 | Nuomeng/诺盟 | 64° | 39.2° | The pipeline is blocked and cannot be adjusted./管路遮挡，无法调整 |

Risk Analysis:

风险分析：

Specific risks: Assess the risk that the dead zone of hydrops becomes a hotbed for microbial colonization. The solvents of related valves involved in this production transfer are all organic solvents, which are not substrates for promoting microbial growth, and the risks can be eliminated;

具体风险，评估积液死区成为微生物定植温床滋生风险，本次生产转移所涉及相关阀门的溶剂，均为有机溶剂，是非促微生物生长基质，风险可排除；

Product Yield Loss Risk: After material piping transfer is completed, process solvent flushing and nitrogen purging are used; since the process piping itself has a slope, the loss risk is low;

产品收率损失风险，物料管路转移结束后使用工艺溶剂进行淌洗，氮气吹扫，工艺管路本身存在坡度，损失风险较低；

Risk Assessment of Residual Finished Products/Materials Unable to Be Discharged from Accumulated Liquid Prolonged Immersion of the Diaphragm (EPDM/PTFE material), causing swelling, hardening, cracking, and shortened service life. Since this usage period is short, only Demo batch production is executed, and immediately after completion corresponding cleaning of equipment and pipelines is performed; there is no corresponding risk;

积液中残留的成品/物料无法排出积液长期浸泡隔膜的风险评估，（EPDM/PTFE材质），导致溶胀、硬化、开裂，使用寿命缩短，本次使用周期较短，仅执行Demo批次生产，结束后立即进行对应的设备及管线的清洁，无对应风险；

Control Measures:

控制措施：

Short-term Measures: Execute according to the risk assessment plan to support Demo batch production. Timely complete drainage through process solvent flushing and nitrogen purging; for cleaning, disassemble non-conforming diaphragm valves for visual inspection; corresponding risks are controllable.

短期措施：按照风险评估的方案执行，支持Demo批次生产。通过工艺溶剂淌洗、氮气吹扫，及时排尽；清洗上，拆卸不满足的隔膜阀进行目视检查，对应风险可控。

Long-term Measures: Before the Pre-PPQ batch, carry out equipment and piping modification to structurally eliminate the diaphragm valve installation angle problem. And conduct re-validation confirmation of piping and equipment.

长期措施：在Pre-PPQ批次前进行设备管路改造，从结构上消除隔膜阀安装角度问题。并进行管路和设备的再次验证确认。

Targeted evaluation form FMEA/针对性FMEA评估表：

| Failure mode/失效模式 | Potential impact/潜在影响 | Before taking measures/措施前 |  |  |  |  | Control measure/控制措施 | After the measures/措施后 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | S | P | D | RPN | Risk level/风险等级 |  | S | P | D | RPN | Risk level/风险等级 |
| Liquid accumulation at the bottom of valve cavity leads to microbial colonization./阀腔底部积液导致微生物定植 | May breed microorganisms/可能滋生微生物 | 2 | 3 | 3 | 18 | 中风险 | Clear material classification; Dismantle the unsatisfactory diaphragm valve for visual inspection; Increase wipe sampling (physicochemical/microbial)/明确物料分类；拆卸不满足的隔膜阀进行目视检查；增加擦拭取样（理化/微生物） | 2 | 2 | 2 | 8 | Low risk/低风险 |
| Long-term immersion swelling, hardening and cracking of diaphragm/隔膜长期浸泡溶胀、硬化、开裂 | Affect the life of the valve/影响阀门寿命 | 2 | 3 | 3 | 18 | 中风险 | Short service life, only Demo batch; Clean immediately after the end; Pre-PPQ transformation/使用周期短，仅Demo批次；结束后立即清洁；Pre-PPQ前改造 | 2 | 1 | 2 | 4 | Low risk/低风险 |

Conclusion:

结论：

The existing equipment can support Demo batch production. After the Demo batch, re-design and modify non-conforming piping, then conduct validation after modification, ensuring this non-compliance item is resolved before Pre-PPQ.

现有设备可以支持Demo批次的生产，Demo批次后对不合格的管路进行重新设计改造，改造后进行验证，确保在Pre-PPQ前解决该不满足项。

4.Conclusion /小结

Through the above risk analysis, methods such as flushing, nitrogen purging, disassembly cleaning confirmation can reduce the risk of non-compliance items in the 139788 step3 equipment/piping validation to low risk, supporting Demo batch production; after the Demo batch, re-design and modify non-conforming piping, then conduct validation after modification, ensuring this non-compliance item is resolved before Pre-PPQ.

经过以上风险分析，通过淌洗、氮气吹扫、拆卸清洗确认等方式可以将139788 step3设备管线验证中不满足项的风险降低为低风险，支持Demo批次的生产；Demo批次后对不合格的管路进行重新设计改造，改造后进行验证，确保在Pre-PPQ前解决该不满足项。

5.Revision History /修订历史

| Effective Date/生效日期 | Doc. No. and version/ 文件编号及版本号 | Document Changes/ 修订内容 | Justification/ 说明 |
| --- | --- | --- | --- |
| Date of the last signatory/最后签字日期 | RA-TJ42026063.01 | New version/新版本 | In this risk assessment, a systematic risk assessment is carried out for the unsatisfied items in the quality inspection plan & report (SVP-TJ4-183.01-004) of the material conveying pipeline of 139788 step3 equipment./本风险评估针对139788 step3设备物料输送管路质量检测方案&报告（SVP-TJ4-183.01-004）不满足项开展系统性风险评估。 |