Risk Assessment of Non-conformances Identified in the Material Transfer Piping Quality Inspection Protocol & Report for 139788 Step 3 Equipment, TJ4 Site /

TJ4厂区139788 step3设备物料输送管路质量检测方案&报告不满足项风险评估

Document No. /文件编号：RA-TJ42026063.01

| Prepared by /起草人 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Fengjiang Li/李丰江 (Junior Engineer, Production/初级工程师，生产部) | Signature/ 签名 |  | Date/ 日期 |  |
| Reviewed by/复核人 |  |  |  |  |
| Xingtao Fan/范兴涛 (Senior Director, Production/高级主管，生产部) | Signature/签名 |  | Date/日期 |  |
| Hui Ma /马辉 (Senior Director, Production/高级主管，生产部) | Signature/签名 |  | Date/日期 |  |
| Meijia Liu/刘美佳 (Senior Director, QA/高级主管，QA) | Signature/签名 |  | Date/日期 |  |
| Approved by/审批人 |  |  |  |  |
| Shenghui Yu/于生辉 (Deputy General Manager, QA/副总经理，QA) | Signature/签名 |  | Date/日期 |  |

Table of Contents/目录

1. Objective/目的	3

2. Scope /范围	3

3. Risk assessment /风险分析	3

3.1 Non-conformance 1: Non-BPE (ISO) Piping in the 139788 Step 3 Preparative Buffer Preparation and Preparative Chromatography Systems	4

3.1 不满足项1：139788 step3制备配液系统及制备系统管路是非BPE管路的评估；	4

3.2 Non-conformance 2: Tees, Crosses and Other Branches Not Meeting the 2D Dead-Leg Requirement	9

3.2 不满足项2：管路多个三通、四通等位置不满足2D的情况；	9

3.3 Non-conformance 3: Diaphragm Valves Not Installed at the Self-Draining Angle	13

3.3 不满足项3：隔膜阀安装角度不满足自排尽的情况。	13

4. Conclusion /小结	15

5. Revision History /修订历史	16

1. Objective/目的

Asymchem Life Science (Tianjin) Co., Ltd. (No. 265, South Street, Economic and Technological Development Zone, Binhai New Area, Tianjin, China) (hereinafter referred to as the "TJ4 Site") is a multi-purpose manufacturing plant designed for the production of various intermediates and APIs. The equipment and facilities employed for the production of intermediates and APIs are non-dedicated and are adaptable for campaign-based manufacturing of multiple products./

凯莱英医药集团（天津）股份有限公司（中国天津市滨海新区经济技术开发区南大街265号）（简称TJ4厂区）是一家多用途生产工厂，旨在生产不同的中间体和API。用于生产中间体和 API 的设备和设施是非专用的，可适配多品种产品阶段性生产。

The purpose of this risk assessment is to systematically assess the non-conformances identified in the Material Transfer Piping Quality Inspection Protocol & Report (SVP-TJ4-183.01-004) for 139788 Step 3 equipment.
      /

该风险评估的目的是对139788 step3设备物料输送管路质量检测方案&报告（SVP-TJ4-183.01-004）不满足项开展系统性评估。

2. Scope /范围

This risk assessment applies to the systematic assessment of the non-conformances identified in the Material Transfer Piping Quality Inspection Protocol & Report (SVP-TJ4-183.01-004) for 139788 Step 3 at Asymchem Life Science (Tianjin) Co., Ltd. (No. 265, South Street, Economic and Technological Development Zone, Binhai New Area, Tianjin, China) (hereinafter referred to as the "TJ4 Site"). The non-conformances fall into three areas that do not meet the corresponding ASME BPE requirements: (1) non-BPE (ISO) piping used in the 139788 Step 3 preparative buffer preparation system and preparative chromatography system; (2) tees, crosses and vessel nozzles on equipment and piping not meeting the 2D dead-leg requirement (L/D ≤ 2); and (3) diaphragm valves not installed at the self-draining angle.
      
      
      
      
      
      
      /

本评估文件适用于凯莱英医药集团（天津）股份有限公司（中国天津市滨海新区经济技术开发区南大街265号）（简称TJ4厂区）的139788 step3物料输送管路质量检测方案&报告（SVP-TJ4-183.01-004）不满足项开展系统性评估。主要是三个方面的不能满足对应BPE标准要求，分别是：1.139788 step3制备配液系统及制备系统管路是非BPE管路的评估；2.设备、管路多个三通、四通、罐口不满足2D的情况，3.隔膜阀安装角度不满足自排尽的情况。

3. Risk assessment /风险分析

The 139788 Step 3 process piping is used mainly to transfer reaction mixtures and process solutions between equipment items in this step, allowing process solutions to be transferred in a closed system. The piping is mainly 316L stainless steel of various sizes, with some Hastelloy. Most process lines use sanitary clamp (tri-clamp) connections and include standard straight spools less than 2 m long. The piping system also includes standard clamp elbows, tees, crosses, etc., and valves, flowmeters, pumps and hoses are installed to control material transfer and minimize residues. The piping is effectively cleaned during and after project batches using the applicable cleaning methods, to prevent cross-contamination and control bioburden and endotoxin. Some hoses are PTFE-lined with a smooth internal surface, meeting material compatibility and residue control requirements.

139788step3工艺管路主要是该步骤各个设备之间用于体系或溶液转移使用，工艺溶液在管道内可以实现密闭转移。目前管路的材质主要是不同规格的316L不锈钢的材质，部分为哈氏合金材质，工艺管路多数采用快开的连接方式，含标准的长度小于2m的直管，管路系统中还包含有对应标准快开弯头、三通、四通等部件，管路中设置有阀门、流量计、泵、软管等设计，以实现物料的转移控制，并最大程度的控制残留。项目批次内、结束后通过对应的清洗方法，实现对管路的有效清洁，避免交叉污染、控制微生物和内毒素负载。其中部分软管为内衬四氟且内表面光滑的形式，可以满足物料的材质兼容性要求残留的控制要求。

In the 139788 Step 3 process piping, ISO-standard piping is manually welded, while BPE piping is orbitally (automatically) welded. All piping is passivated prior to use and qualified per the Material Transfer Piping Quality Inspection Protocol & Report (SVP-TJ4-183.01-004). This document performs an FMEA on the three non-conformances to ensure that the associated risks are controlled, and defines short-term and long-term measures./

139788step3工艺管路中ISO标准管路采用手动焊接的形式，BPE管路采用自动焊接的形式，对应管道均进行对应的使用前的钝化工作及管道验证工作（物料输送管路质量检测方案&报告（SVP-TJ4-183.01-004）），本文件主要是针对三个方面的不满足的情况进行FMEA风险分析，以确保对应风险可控，并制定短期和长期的措施。

FMEA Scoring Criteria:/FMEA评分标准说明：

· Severity (S): 1 = Negligible; 2 = Minor impact (no effect on final product quality or safety); 3 = Moderate impact (rework required/reduced yield); 4 = Severe impact (affects critical quality attributes of the product/leads to batch rejection); 5 = Catastrophic (impact on product quality/patient safety, or regulatory non-compliance).

严重度（S）：1=可忽略；2=轻微影响（不影响最终产品质量和安全性）；3=中等影响（需返工/收率下降）；4=严重影响（影响产品关键质量属性/导致停批）；5=灾难性（质量安全/法规违规）。

· Probability of Occurrence (P): 1 = Rare (<1%); 2 = Unlikely (1–5%); 3 = Occasional (5–10%); 4 = Frequent (10–30%); 5 = Very frequent (>30%).

发生概率（P）：1=极少发生（<1%）；2=不太可能发生（1%-5%）；3=偶尔发生（5-10%）；4=经常发生（10-30%）；5=频繁发生（>30%）。

· Detectability (D): 1 = Almost certain detection (e.g., 100% borescope inspection plus physicochemical testing); 2 = High likelihood of detection (e.g., visual inspection at a high sampling rate plus physicochemical testing); 3 = Moderate likelihood of detection (e.g., visual inspection on a sampling basis); 5 = Almost impossible to detect (e.g., only by final product testing).

可检测度（D）：1=几乎肯定能检出（如100%内窥镜+理化检测）；2=大概率能检出（如高比例抽检目视＋理化检测）；3=有中等机会检出（如抽检目视）；5=几乎无法检出（如仅靠终产品检验）。

· Risk grade determination: RPN ≤ 12 (low risk, acceptable); 12 < RPN ≤ 24 (medium risk, need control measures); RPN > 24 (high risk, must be rectified/require special approval from QA).

风险等级判定：RPN ≤ 12（低风险，可接受）；12 < RPN ≤ 24（中风险，需控制措施）；RPN > 24（高风险，必须整改/需QA特批）。

（RPN＝S×P×D）

3.1 Non-conformance 1: Non-BPE (ISO) Piping in the 139788 Step 3 Preparative Buffer Preparation and Preparative Chromatography Systems

3.1 不满足项1：139788 step3制备配液系统及制备系统管路是非BPE管路的评估；

Description:

具体情况：

Due to the long lead time of BPE tubing, ISO piping was used on an interim basis for the early Demo batches of 139788 Step 3. After the BPE tubing arrives, the piping will be re-fabricated and re-installed using BPE tubing. This document compares the existing ISO piping with ASME BPE requirements and assesses whether it is suitable for production use.

本次139788step3管路因BPE管路到货周期较长，临时进行前期Demo批次的使用，待后续BPE管路到货后进行重新制作安装，对应现有的ISO管路和BPE管路进行整体的对比和风险分析，确认是否满足项目生产使用。

Piping List:

具体管路清单：

| Line No./管路编号 | Size/规格 | Material/材质 | Applicable Standard/执行标准 |
| --- | --- | --- | --- |
| 139788-step3B-P06 | DN25 | 316L | ISO |
| 139788-step3B-P07 | DN25 | 316L | ISO |
| 139788-step3B-P04 | DN25 | 316L | ISO |
| 139788-step3B-P01 | DN50 | 316L | ISO |
| 139788-step3B-P02 | DN25 | 316L | ISO |
| 139788-step3B-P03 | DN25 | 316L | ISO |
| 1211-FD01-P01 | DN40/ DN25（Reducer/ 变径） | 316L | ISO |
| 1211-AT01-P01 | DN25 | 316L | ISO |
| Acetonitrile line/ 乙腈管路 | DN50 | 316L | ISO |
| 1211-HPPC03-T02-P02 | DN25 | 316L | ISO |
| 1211-HPPC03-T04-P01 | DN25 | 316L | ISO |
| 1211-HPPC03-T05-P02 | DN25 | 316L | ISO |
| 1211-HPPC03-T02-P04 | DN40 | 316L | ISO |
| 1211-HPPC03-T06-P03 | DN25 | 316L | ISO |
| 1211-HPPC03-T05-P01 | DN25 | 316L | ISO |
| 1211-HPPC03-AT01-P02 | DN25 | 316L | ISO |
| 1211-HPPC03-T01-P04 | DN25 | 316L | ISO |
| 1211-HPPC03-T01-P03 | DN25 | 316L | ISO |
| 1211-HPPC03-T02-P03 | DN25 | 316L | ISO |
| 1211-HPPC03-AT04-P03 | DN25 | 316L | ISO |
| 139788-step3A-P06 | DN25 | 316L | ISO |
| 1211-HPPC03- P04 | DN25 | 316L | ISO |
| 1211-HPPC03- P01 | DN25 | 316L | ISO |
| 139788-step3A-P04 | DN25 | 316L | ISO |
| 1211-HPPC03-AT03-P02 | DN25 | 316L | ISO |
| 1211-HPPC03-AT06-P02 | DN25 | 316L | ISO |

Risk Analysis:

风险分析：

A systematic assessment of the core technical requirements, including material, welding, pickling and passivation, and dimensional tolerances, was performed based on ISO tubing standard requirements, with reference to ASME BPE-2026 (Bioprocessing Equipment, June 2026). The assessment covers the following core equipment and facility components: piping, fittings, valves, pumps, and all product-contact surfaces and their surface treatment. The assessment includes the core requirements for material, welding, pickling and passivation, dimensional tolerances and surface finish.

从材质、焊接、酸洗钝化及公差直径等核心技术要求进行系统性评估，依据ISO 标准体系要求，参考ASME BPE-2026（生物工艺设备标准，2026年6月），
      评估涵盖以下核心设备设施组件：管道、管件、阀门、泵，以及与产品接触的所有表面处理环节。评估包涵材质、焊接、酸洗钝化、公差直径、表面光洁度核心要求。

Material Requirements Assessment: All product-contact surfaces use 316L as the baseline; non-product-contact surfaces may be 304/304L. Material test reports (MTRs) including chemical composition are provided for all of the above materials. Requirements are essentially equivalent between ISO and ASME BPE-2026.

材质要求评估：产品接触面均以316L为基准，非接触面可降级至304/304 L，以上相关材料均提供材质证明包含材料含量，ISO和ASME BPE-2026要求基本一致。

Welding Requirements Assessment: Argon shielding gas was tested at 99.997% purity, meeting the shielding gas requirement. Orbital (automatic) welding is preferred; manual welding is used only where orbital welding is not practicable. Internal borescope examination: ≥ 20% of orbital (automatic) welds and 100% of manual welds. The 2D dead-leg rule (L/D ≤ 2) applies. Porosity, undercut, slag inclusions, etc. are not permitted on product-contact surfaces. Requirements are essentially equivalent between ISO and ASME BPE-2026, and ISO tubing is accepted against ASME BPE-2026 acceptance criteria. Welders hold government-issued Special Operations Certificates for welding
      ./

焊接要求评估：焊接气体经过检测99.997%满足氩气保护要求，焊接方法以自动焊接优先为主，手动焊接为辅助，检测比例自动焊缝 ≥20%内窥镜检查，手动焊缝100%内窥镜检查，2D死角规则L/D ≤ 2:1，产品接触面不允许气孔、咬边、焊渣等要求，ISO和ASME BPE-2026要求基本一致，且针对ISO标准管材的验收以ASME BPE-2026的要求为标准。焊接人员资质为政府特种作业操作证。

The following assesses the gaps arising from accepting ISO tubing against ASME BPE criteria. For welding, ISO tubing differs from BPE requirements in sulfur content, dimensional tolerances and end-face quality, which may cause inconsistent orbital weld-pool flow, incomplete fusion, porosity, hot cracking or fit-up misalignment. For internal surface roughness, ISO tubing usually specifies only an Ra value, whereas ASME BPE defines surface finish designations SF1–SF6; higher roughness will reduce CIP/SIP effectiveness. To address these risks, the following controls are applied: 100% verification of tube-end OD, wall thickness and ovality to control fit-up misalignment; re-qualification of the welding procedure (WPS/PQR) using tubing from the same heat/lot, with fixed weld parameters and every weld recorded in the weld log/weld map; borescope inspection of 20% of orbital welds and 100% of manual welds; and verification of internal surface roughness against the supplier's roughness test report, accepted per ASME BPE. Combined with cleaning validation and surface (swab) sampling monitoring, these controls effectively reduce the welding-defect and cleaning risks arising from the differences between ISO tubing and the ASME BPE standard. Therefore, this approach is technically feasible, and the residual risk from these differences is acceptable under the stated controls
      
      ./

针对采用ISO标准管材按ASME BPE验收的管道系统不一致方面评估。焊接方面，ISO管材在硫含量、尺寸公差和端面质量与BPE要求存在偏差，可能导致轨道焊熔池流动性不足、未熔合、气孔、热裂纹或组对错边等缺陷。内壁粗糙度方面，ISO管材通常仅规定Ra值，而BPE对表面光洁度有SF1–SF6体系化要求，粗糙度偏高会影响CIP/SIP效果。针对上述风险采取以下控制措施：100%复核管端外径、壁厚及椭圆度，控制组对错边；使用本批管材重新进行焊接工艺评定，锁定焊接参数并记录每道焊口；自动焊内窥镜抽检比例20%，手工焊100%内窥镜检查；内壁粗糙度由厂家提供粗糙度检测报告，我司以BPE标准进行核查验收，结合清洁验证及表面取样监测，可有效降低ISO管材与BPE标准差异带来的焊接缺陷和清洁风险。因此，该方案在受控条件下技术可行，差异风险可接受。

Pickling and Passivation Requirements Assessment: Pickling and passivation protocols, execution records, post-passivation test results and surface finish specifications are available. Requirements are essentially equivalent between ISO and ASME BPE-2026.

酸洗钝化要求评估：有酸洗钝化方案、酸洗钝化记录、酸洗钝化后检测结果和抛光度标准，ISO和ASME BPE-2026要求基本一致。

Tolerance and Diameter Requirements Assessment: Piping uses sanitary clamp (tri-clamp) connections; piping slope is ≥ 1%; product-contact surface roughness is Ra ≤ 0.4 µm. Requirements are essentially equivalent between ISO and ASME BPE-2026. Pipe diameter, tolerance, wall thickness, etc. are selected according to the requirements of each process point, using tubing that meets ISO or ASME BPE-2026 process requirements; the process risk is acceptable./

公差与直径要求评估：管道连接卡箍快接、管道坡度满足≥1%、直接接触产品内表面粗糙度要求满足Ra≤0.4 μm
      ，ISO和ASME BPE-2026要求基本一致，管道直径、公差、壁厚等结合工艺的不同点位选用满足ISO或ASME BPE-2026工艺需求的管材，工艺风险可接受。

Control Measures:

控制措施：

Short-term Measures: The ISO piping shall be managed under the same requirements as BPE piping, to support production of the 139788 Step 3 Demo batches
      ./

短期措施：管路整体管理要求同BPE管路一致，支持139788 step3 Demo批次的生产。

Long-term Measures: Complete redesign, installation and qualification of BPE piping before 139788 Step 3 Pre-PPQ; this piping will then be dedicated to the project./

长期措施：在139788 step3 Pre-PPQ前完成BPE管路的重新设计及安装验证工作，后续作为该项目的专用管路。

FMEA Worksheet/针对性FMEA评估表：

| Failure Mode/失效模式 | Potential Effect/潜在影响 | Pre-mitigation/ 措施前 |  |  |  |  | Control Measures/控制措施 | Post-mitigation (Residual)/ 措施后 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | S | P | D | RPN | Risk Level/风险等级 |  | S | P | D | RPN | Risk Level/风险等级 |
| Misalignment and incomplete fusion at ISO-to-BPE welds/ ISO/BPE混杂焊接产生错边、未熔合 | Compromised weld quality; may create uncleanable crevices/ 影响焊接质量，可能导致清洁死角 | 2 | 3 | 3 | 18 | Medium risk/中风险 | 100% verification of tube-end dimensions to control misalignment; 100% borescope inspection of ISO-to-BPE butt welds; re-qualification of the welding procedure/ 100%复核管端尺寸，控制错边；ISO-BPE对接焊缝100%内窥镜检查；重新进行焊接工艺评定 | 1 | 2 | 2 | 4 | Low risk/低风险 |
| Sulfur content of ISO tubing differs from ASME BPE requirements, affecting weldability/ ISO管道硫含量与BPE标准存在差异，影响焊接质量 | May cause inconsistent weld-pool flow, porosity, hot cracking and incomplete fusion, affecting weld quality and increasing cleaning risk/ 可能导致熔池流动性不足、气孔、热裂纹、未熔合等缺陷，影响焊缝质量及清洁风险 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Verify sulfur content against the tubing MTRs and retest per heat if necessary; 100% verification of tube-end dimensions to control misalignment; re-qualify the welding procedure using tubing from the same heat/lot and fix the weld parameters; 100% borescope inspection of ISO-to-BPE butt welds; borescope inspection of 20% of orbital welds and 100% of manual welds/ 核查管材材质证书中硫含量，必要时按批次复测；100%复核管端尺寸，控制错边；使用本批管材重新进行焊接工艺评定，锁定焊接参数；ISO-BPE对接焊缝100%内窥镜检查；自动焊内窥镜抽检20%，手工焊100%内窥镜检查 | 2 | 2 | 2 | 8 | Low risk/低风险 |
| Differences in internal surface roughness reduce CIP/SIP effectiveness/ 内壁粗糙度差异影响CIP/SIP效果 | May reduce cleaning effectiveness/ 可能影响清洁效果 | 2 | 1 | 2 | 4 | Low risk/低风险 | Internal surface roughness is verified against the supplier's roughness test report and accepted per ASME BPE, combined with cleaning validation and surface (swab) sampling monitoring./ 内壁粗糙度由厂家提供粗糙度检测报告，我司以BPE标准进行核查验收，结合清洁验证及表面取样监测。 | 2 | 1 | 2 | 4 | Low risk/低风险 |

Conclusion:

结论：

After systematic evaluation, all tubing is accepted against ASME BPE-2026 requirements. ASME BPE-2026 provides a complete, executable framework covering welding procedure qualification, welder qualification and weld acceptance criteria, as well as core management elements such as materials, welding methods and qualifications, basic passivation requirements, drainage slope, dead-leg rules and surface roughness. The residual risk from the differences is controlled; ASME BPE-2026 is therefore applied directly as the acceptance basis, and the risk to the project is low./

经系统评估，以ASME BPE-2026要求标准对所有的管材进行验收，在焊接工艺评定、焊工资格、焊接验收等级方面形成了完整的标准群，提供了可执行的主框架，覆盖材质、焊接方法与资格、钝化基本要求、排水坡度、死角规则与表面粗糙度等核心管理要素，差异风险可控，故可直接作为执行依据，项目使用风险较低。

3.2 Non-conformance 2: Tees, Crosses and Other Branches Not Meeting the 2D Dead-Leg Requirement

3.2 不满足项2：管路多个三通、四通等位置不满足2D的情况；

Description:

具体情况：

According to the ASME BPE standard SD-03 chapter Dead Leg control requirements:/

根据ASME BPE标准SD-03章节死腔（Dead Leg）管控要求：

In hygienic fluid systems, for all non-continuous-flow branches (tee branches, instrument connections, sample ports, drain ports, blind caps, etc.), the ratio of the length L, measured from the inner wall of the main line to the closed end of the branch, to the branch inner diameter D must satisfy L/D ≤ 2 (i.e., the 2D requirement).

洁净流体系统中，所有非连续流支路（三通分支、仪表接口、取样口、排放口、堵头等），从主管路内壁到支路盲端的长度L，与支路自身内径D
      的比值需满足 L/D ≤ 2（即2D要求）

Due to the long lead times of short-outlet tees, T-body valves, zero-static (zero dead-leg) valves, sanitary diaphragm valves, etc., the 139788 Step 3 piping was fabricated with standard (general-purpose) fittings. As a result, some components do not meet the 2D requirement; these were identified during piping qualification and are listed in the table below:

本次139788step3管路因短径三通、T型阀、零静态阀门、GMP隔膜阀等货期较长，使用一般配件进行管路的制作，存在部分部件不能满足2D的情况，在管路验证过程中进行识别，具体清单见下表：

| Component Tag No./部件号 | Acceptance Criterion/使用原则 (mm:mm) | L=L0+e1 | D=d0-2e2 | L/D |
| --- | --- | --- | --- | --- |
| TJ4S-1211-FD01-V97 | L/D≤2 | 137.45mm | 27.17mm | 4.83 |
| TJ4S-1211-R01-VS4 | L/D≤2 | 130.15mm | 22.06mm | 5.89 |
| TJ4S-1211-AT02-V23 | L/D≤2 | 124.66mm | 13.80mm | 9.03 |
| TJ4S-1211-AT02-V24 | L/D≤2 | 109.40mm | 12.88mm | 8.49 |
| TJ4S-1211-HPP/03-AT01-V15 | L/D≤2 | 118.74mm | 25.23mm | 4.70 |
| TJ4S-1211-HPP/03-T03-V21 | L/D≤2 | 143.80mm | 22.01mm | 6.53 |
| TJ4S-1211-HPP/03-AT04-V22 | L/D≤2 | 120.27mm | 25.73mm | 4.67 |
| TJ4S-1211-HPP/03-AT04-V24 | L/D≤2 | 119.97mm | 25.87mm | 4.64 |
| TJ4S-1211-TFF02-V31 | L/D≤2 | 123.25mm | 22.14mm | 5.56 |
| TJ4S-1211-HPP/03-AT02-V15 | L/D≤2 | 118.54mm | 26.07mm | 4.54 |
| TJ4S-1211-HPP/03-AT02-V18 | L/D≤2 | 86.09mm | 12.25mm | 7.02 |
| TJ4S-1211-HPP/03-AT02-V14 | L/D≤2 | 118.74mm | 25.23mm | 4.70 |
| TJ4S-1211-HPP/03-T06-V09 | L/D≤2 | 118.98mm | 25.72mm | 4.60 |
| TJ4S-1211-HPP/03-T06-V17 | L/D≤2 | 120.10mm | 25.86mm | 4.64 |
| TJ4S-1211-TFF02-V105 | L/D≤2 | 101.59mm | 13.25mm | 7.66 |
| LY2607062J5 | L/D≤2 | 169.15mm | 25.24mm | 6.54 |
| LY260706226 | L/D≤2 | 172.23mm | 26.90mm | 6.40 |
| Y126070624 | L/D≤2 | 193.64mm | 26.77mm | 7.42 |
| CZH031507 | L/D≤2 | 198.08mm | 27.45mm | 7.21 |
| CZH031508 | L/D≤2 | 165.07mm | 12.56mm | 13.15 |
| CZH081498 | L/D≤2 | 170.73mm | 23.84mm | 6.60 |

Risk Analysis:

风险分析：

When L/D > 2, turbulence in the main line (Reynolds number Re ≥ 3000 under CIP conditions) cannot effectively entrain the fluid in the branch; the branch becomes a stagnant dead leg, the medium cannot circulate and be renewed, and cleaning solution cannot penetrate effectively. This is the underlying cause of the risks below./

当L/D＞2时，主管路的湍流（CIP工况雷诺数Re≥3000）无法有效夹带支路内的流体，支路内部形成静态滞留死区，介质无法循环更新，清洗液、无法有效穿透，是所有风险的根源。

1. Microbial Contamination and Biofilm Risk: Fluid in the dead leg is stagnant. After use, the piping is fully drained at low points, and nitrogen purging further reduces residues. After use, each port is flow-through cleaned to ensure that all flow paths are cleaned. In addition, tees and other components not meeting the 2D requirement are disassembled for visual inspection, and flow-through cleaning and swab sampling of side-branch dead legs are added, reducing the risk to low./

1. 微生物污染与生物膜风险：死区内流体静止，管路在使用完毕后进行低点完全排尽、氮气吹扫进一步降低残留。管路使用完毕后进行各个口的流通式清洗，确保全部路径得到清洗，同时三通等不满足2D的部件进行拆卸进行目视检查确认，增加侧口死区流通式清洗、擦拭取样，可以将风险降到低风险；

2. CIP Cleaning Effectiveness Failure Risk: Turbulence in the main line cannot be transmitted into the dead leg; cleaning solution forms only a weak laminar exchange at the dead-leg inlet and cannot effectively scour the inner wall; residual materials and cleaning agents cannot be fully displaced, resulting in persistent residues. To address this risk, flow-through cleaning of side-branch dead legs is added, and components are visually inspected after disassembly, reducing the risk to low.

2. CIP清洗有效性失效风险：主管路的湍流无法传递至死区内部，清洗液仅能在死区入口形成微弱的层流交换，无法有效冲刷内壁；残留物料、清洁剂无法被完全置换，形成永久残留。根据该风险，增加侧口死区的流通式清洗，并做拆卸下来后的目视检查确认，可以将风险降到低风险。

3. Product Quality and Yield Risk: Product retained in the dead leg cannot be discharged with the main line and remains after batch completion, causing variability in critical quality attributes (CQAs). Product hold-up also reduces yield. To address this risk, the piping is rinsed with process solvent and purged with nitrogen after project use.

3. 产品质量与收率风险：死区内滞留的产品物料无法随主管路排出，批次结束后残留，造成关键质量属性波动。产品滞留损失，产品收率下降。根据该风险特征，项目使用结束后进行工艺溶剂的淌洗、氮气吹扫，避免对应风险。

4. Equipment Corrosion and Maintenance Risk: Liquid retained in the dead leg for long periods degrades the internal surface finish of hygienic piping (Ra ≤ 0.4 µm), causing pitting and crevice corrosion; corrosion products further aggravate hold-up and contamination. To address this risk, the piping is drained promptly after material transfer and cleaning, and because the materials in this project are non-corrosive, the risk is low.

4. 设备腐蚀与运维风险：液体在死区内长期滞留，破坏卫生级管路内表面光洁度（Ra≤0.4μm），引发点蚀、缝隙腐蚀；腐蚀产物进一步加剧滞留与污染。针对该风险在物料以及清洗转移结束后进行及时排尽，且本项目中对应物料无腐蚀性，风险较低。

Control Measures:

控制措施：

Short-term Measures: Execute per this risk assessment to support Demo batch production. Drain promptly by process solvent rinsing and nitrogen purging; for cleaning, flow-through clean each port and disassemble components for visual inspection; the associated risks are controlled./

短期措施：按照风险评估的方案执行，支持Demo批次生产。通过工艺溶剂淌洗、氮气吹扫，及时排尽；清洗上，各个口流通式清洗，并拆卸进行目视检查，对应风险可控。

Long-term Measures: Before the Pre-PPQ batches, modify the equipment and optimize dimensions: shorten non-conforming branches to strictly meet L/D ≤ 2; where a branch cannot be shortened, replace it with zero-dead-leg valves/tees or flush-mounted clamp fittings to structurally eliminate hold-up cavities. Then re-qualify the piping and equipment.

长期措施：在Pre-PPQ批次前进行设备改造，尺寸优化改造：对超标支管进行截短，严格控制L/D≤2；无法截短的位置更换为零死区三通、夹装式齐平接头，从结构上消除滞留腔。并进行管路和设备的再次验证确认。

FMEA Worksheet/针对性FMEA评估表：

| Failure Mode/失效模式 | Potential Effect/潜在影响 | Pre-mitigation/ 措施前 |  |  |  |  | Control Measures/控制措施 | Post-mitigation (Residual)/ 措施后 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | S | P | D | RPN | Risk Level/风险等级 |  | S | P | D | RPN | Risk Level/风险等级 |
| Dead-leg hold-up leads to microbial growth (aqueous lines)/死区滞留导致微生物滋生（水相管路） | May breed microorganisms/可能滋生微生物 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Identify all aqueous lines; add flow-through cleaning of side-branch dead legs; add swab sampling/ 识别水相管路清单；增加侧口死区流通式清洗；增加擦拭取样 | 2 | 2 | 2 | 8 | Low risk/低风险 |
| Failure of CIP cleaning effectiveness and material residue /CIP清洗有效性失效、物料残留 | Material residue, affecting cleaning./物料残留，影响清洁 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Disassemble and visually inspect components not meeting the 2D requirement; add physicochemical testing of swab samples; process solvent rinse and nitrogen purging/拆卸不满足2D部件目视检查；增加擦拭取样理化检测；工艺溶剂淌洗、氮气吹扫 | 2 | 2 | 2 | 8 | Low risk/低风险 |
| Prolonged liquid hold-up causes corrosion/ 长期滞留导致管路腐蚀 | May corrode the piping/可能腐蚀管路 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Drain promptly after use; materials are non-corrosive; periodic inspection/ 使用后及时排尽；物料无腐蚀性；定期检查 | 2 | 1 | 2 | 4 | Low risk/低风险 |

Conclusion:

结论：

The existing equipment can support Demo batch production. After the Demo batches, the non-conforming piping will be redesigned, modified and re-qualified, ensuring this non-conformance is resolved before Pre-PPQ.

现有设备可以支持Demo批次的生产，Demo批次后对不合格的管路进行重新设计改造，改造后进行验证，确保在Pre-PPQ前解决该不满足项。

3.3 Non-conformance 3: Diaphragm Valves Not Installed at the Self-Draining Angle

3.3 不满足项3：隔膜阀安装角度不满足自排尽的情况。

Description:

具体情况：

This assessment is based on ASME BPE (hygienic piping shall be sloped ≥ 1%, and valves shall follow the piping slope to be self-draining) and China GMP (piping design and installation shall avoid dead legs and blind ends to prevent microbial growth and ensure complete drainage of the system). The non-conformance identified during qualification arises because weir-type sanitary diaphragm valves drain by gravity only when installed at the manufacturer's specified drain angle. When the installation angle is not met (horizontal with no slope, insufficient slope or reverse slope), persistent liquid hold-up forms at the bottom of the valve cavity, which is the underlying cause of the risks below. The installation angle of each valve follows the manufacturer's manual and was measured and confirmed individually during piping qualification. Diaphragm valves identified during qualification as not meeting the requirement are listed below:

本次评估基于ASME BPE 标准：洁净管路短管坡度≥1%，阀门需顺应管路坡度实现自排净；中国GMP：管道设计安装应避免死角、盲管，防止微生物滋生，确保系统完全排放。在本次验证中隔膜阀不满足的本质是堰式结构卫生级隔膜阀的自排净依赖重力作用，安装角度不达标（水平无倾斜、倾斜不足、反向倾斜）时，阀腔底部会形成永久性积液死区，是所有风险的根源。具体阀门的安装角度依据厂家设备说明书执行，在管道验证中进行逐一测量确认。以下是在验证中识别的不满足标准的隔膜阀清单：

| No./ 序号 | Valve Tag No./阀门编号 | Manufacturer/厂家 | Required Drain Angle/目标角度 | As-installed Angle/当前角度 | Remarks/备注 |
| --- | --- | --- | --- | --- | --- |
| 1 | TJ4S-1211-TFF02-V60 | Nuomeng/诺盟 | 60° | 40.4° | Obstructed by adjacent piping; cannot be adjusted./管路遮挡，无法调整 |
| 2 | TJ4S-1211-TFF02-V123 | Nuomeng/诺盟 | 60° | 38.9° | Obstructed by adjacent piping; cannot be adjusted./管路遮挡，无法调整 |
| 3 | TJ4S-1211-HPPC03-AT05-V29 | Nuomeng/诺盟 | 60° | -90° | Valve installed inverted, flush against the top plate./阀门倒垂，紧贴顶板 |
| 4 | TJ4S-1211-HPPC03-AT06-V19 | Nuomeng/诺盟 | 60° | -90° | Valve installed inverted, flush against the top plate./阀门倒垂，紧贴顶板 |
| 5 | TJ4S-1211-HPPC03-AT06-V20 | Nuomeng/诺盟 | 60° | -90° | Valve installed inverted, flush against the top plate./阀门倒垂，紧贴顶板 |
| 6 | TJ4S-1211-HPPC03-AT06-V21 | Nuomeng/诺盟 | 60° | -90° | Valve installed inverted, flush against the top plate./阀门倒垂，紧贴顶板 |
| 7 | TJ4S-1211-HPPC03-AT06-V22 | Nuomeng/诺盟 | 60° | -90° | Valve installed inverted, flush against the top plate./阀门倒垂，紧贴顶板 |
| 8 | TJ4S-1211-R01-V03 | Nuomeng/诺盟 | 71° | 90° | Valve installed vertically, flush against the top plate./阀门垂直，紧贴顶板 |
| 9 | TJ4S-1211-R01-V24 | Nuomeng/诺盟 | 64° | 90° | Valve installed vertically, flush against the top plate./阀门垂直，紧贴顶板 |
| 10 | TJ4S-1211-R01-V25 | Nuomeng/诺盟 | 64° | 90° | Valve installed vertically, flush against the top plate./阀门垂直，紧贴顶板 |
| 11 | TJ4S-1211-R01-V54 | Nuomeng/诺盟 | 64° | 39.2° | Obstructed by adjacent piping; cannot be adjusted./管路遮挡，无法调整 |

Risk Analysis:

风险分析：

Microbial Colonization Risk: The risk of microbial colonization in liquid hold-up in the valve cavity was assessed. The solvents passing through the affected valves in this production are all organic solvents, which do not support microbial growth; this risk is considered negligible;

具体风险，评估积液死区成为微生物定植温床滋生风险，本次生产转移所涉及相关阀门的溶剂，均为有机溶剂，是非促微生物生长基质，风险可排除；

Product Yield Loss Risk: After material transfer, the piping is rinsed with process solvent and purged with nitrogen; because the process piping is itself sloped, the risk of loss is low;

产品收率损失风险，物料管路转移结束后使用工艺溶剂进行淌洗，氮气吹扫，工艺管路本身存在坡度，损失风险较低；

Diaphragm Degradation Risk: Prolonged immersion of EPDM/PTFE diaphragms in retained product or material that cannot be drained may cause swelling, hardening and cracking, shortening diaphragm life. Because the period of use is short (Demo batch production only) and the equipment and piping are cleaned immediately afterwards, this risk is considered negligible;

积液中残留的成品/物料无法排出积液长期浸泡隔膜的风险评估，（EPDM/PTFE材质），导致溶胀、硬化、开裂，使用寿命缩短，本次使用周期较短，仅执行Demo批次生产，结束后立即进行对应的设备及管线的清洁，无对应风险；

Control Measures:

控制措施：

Short-term Measures: Execute per this risk assessment to support Demo batch production. Drain promptly by process solvent rinsing and nitrogen purging; for cleaning, disassemble non-conforming diaphragm valves for visual inspection; the associated risks are controlled.

短期措施：按照风险评估的方案执行，支持Demo批次生产。通过工艺溶剂淌洗、氮气吹扫，及时排尽；清洗上，拆卸不满足的隔膜阀进行目视检查，对应风险可控。

Long-term Measures: Before the Pre-PPQ batches, modify the equipment and piping to structurally eliminate the diaphragm valve installation angle issue. Then re-qualify the piping and equipment.

长期措施：在Pre-PPQ批次前进行设备管路改造，从结构上消除隔膜阀安装角度问题。并进行管路和设备的再次验证确认。

FMEA Worksheet/针对性FMEA评估表：

| Failure Mode/失效模式 | Potential Effect/潜在影响 | Pre-mitigation/ 措施前 |  |  |  |  | Control Measures/控制措施 | Post-mitigation (Residual)/ 措施后 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | S | P | D | RPN | Risk Level/风险等级 |  | S | P | D | RPN | Risk Level/风险等级 |
| Liquid accumulation at the bottom of valve cavity leads to microbial colonization./阀腔底部积液导致微生物定植 | May breed microorganisms/可能滋生微生物 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Classify lines as aqueous or organic; disassemble non-conforming diaphragm valves for visual inspection; add swab sampling (physicochemical/microbial)/明确物料分类；拆卸不满足的隔膜阀进行目视检查；增加擦拭取样（理化/微生物） | 2 | 2 | 2 | 8 | Low risk/低风险 |
| Diaphragm swelling, hardening or cracking due to prolonged immersion/ 隔膜长期浸泡溶胀、硬化、开裂 | Affect the life of the valve/影响阀门寿命 | 2 | 3 | 3 | 18 | Medium risk/中风险 | Limited period of use (Demo batches only); clean immediately after use; modification before Pre-PPQ/ 使用周期短，仅Demo批次；结束后立即清洁；Pre-PPQ前改造 | 2 | 1 | 2 | 4 | Low risk/低风险 |

Conclusion:

结论：

The existing equipment can support Demo batch production. After the Demo batches, the non-conforming piping will be redesigned, modified and re-qualified, ensuring this non-conformance is resolved before Pre-PPQ.

现有设备可以支持Demo批次的生产，Demo批次后对不合格的管路进行重新设计改造，改造后进行验证，确保在Pre-PPQ前解决该不满足项。

4. Conclusion /小结

Based on the above risk analysis, rinsing, nitrogen purging, and disassembly with post-cleaning visual verification reduce the risk of the non-conformances identified in 139788 Step 3 equipment/piping qualification to low, supporting Demo batch production. After the Demo batches, the non-conforming piping will be redesigned, modified and re-qualified, ensuring these non-conformances are resolved before Pre-PPQ.

经过以上风险分析，通过淌洗、氮气吹扫、拆卸清洗确认等方式可以将139788 step3设备管线验证中不满足项的风险降低为低风险，支持Demo批次的生产；Demo批次后对不合格的管路进行重新设计改造，改造后进行验证，确保在Pre-PPQ前解决该不满足项。

5. Revision History /修订历史

| Effective Date/生效日期 | Doc. No. and version/ 文件编号及版本号 | Document Changes/ 修订内容 | Justification/ 说明 |
| --- | --- | --- | --- |
| Date of last signature/最后签字日期 | RA-TJ42026063.01 | Initial issue/新版本 | This risk assessment systematically assesses the non-conformances identified in the Material Transfer Piping Quality Inspection Protocol & Report (SVP-TJ4-183.01-004) for 139788 Step 3 equipment. /本风险评估针对139788 step3设备物料输送管路质量检测方案&报告（SVP-TJ4-183.01-004）不满足项开展系统性风险评估。 |